IRAN PASARGAD

IRAN PASARGAD (WATERMARK PLACEHOLDER)
BITUMEN 60/70 TEST CERTIFICATE
	PROPERTY
	TEST METHOD
	UNIT
	SPECIFICATION
	TYPICAL VALUE

	Penetration at 25°C
	ASTM D5
	0.1 mm
	60–70
	65

	Softening Point (Ring & Ball)
	ASTM D36
	°C
	49–56
	52

	Ductility at 25°C
	ASTM D113
	cm
	Min 100
	>100

	Flash Point (COC)
	ASTM D92
	°C
	Min 250
	290

	Solubility in Trichloroethylene
	ASTM D2042
	%
	Min 99.0
	99.5

	Specific Gravity @25°C
	ASTM D70
	g/cm³
	Report
	1.03

	Loss on Heating
	ASTM D6
	wt %
	Max 0.5
	0.2

	Retained Penetration after TFOT
	ASTM D5
	%
	Min 50
	70

	Increase in Softening Point after TFOT
	ASTM D36
	°C
	Max 9
	4

	Spot Test
	AASHTO T102
	-
	Negative
	Negative



Product Name: Bitumen 60/70
Origin: Iran
Brand: Iran Pasargad
Packaging: New Steel Drum / Jumbo Bag / Bulk
Application: Road Construction & Asphalt Production




